## Slide 1
Z1
Z2
Z3
Z4
Z5
Z6
Z7
Z8
Furnace → Z1 to Z8 | 40 m Walking Beam | Hazira RHF-1
FURNACE SETPOINT
FURNACE SETPOINT
OPTIMISATION
Comparative Schedule Analysis — Current State vs Target State
Source: Hazira_Data_Assessment_filtered.csv + Process_parameter.xlsx
Period: Aug 2025 – Dec 2025 Records: 30,731 slabs + 4,344 hrs process data
Schedules analysed: 5 representative production runs
30,731
Slab Records
4,344
Operational Hours
5
Schedules
8
Zone Model
Hazira Steel Operations · Confidential · April 2026

## Slide 2
ANALYTICAL METHODOLOGY & MODEL FRAMEWORK
📊 DATA SOURCES
Process_parameter.xlsx
4,344 hourly records | Aug 2025 – Jan 2026
Zone temps Z1–Z8, fuel (COREX + NG per zone), AFR, O₂, pressure, damper, chimney FGT
Hazira_Data_Assess…csv
30,731 slab records | Aug 2025 – Dec 2025
Grade, thickness, width, entry temp, actual FCE dropout, target recipe, residence times per zone
Merged dataset
Join on discharge hour
Each slab matched to the hourly furnace conditions at its discharge time — giving true operating context
⚙ THREE-MODEL ARCHITECTURE
M1
Fuel Consumption Model
Fuel_i = intercept_i + slope_i × SP_i (all slopes +ive)
Calibrated: 3,960 hours | All 8 zones independent
Slopes: Z1=25.8 · Z2=34.1 · Z3=38.6 (highest) · Z4=14.2 · Z5–Z8: 0.5–1.6 Nm³/hr per °C SP
M2
FCE Dropout Prediction Model
FCE = 858.3 + Σ(fceCoeff_i × actual_i) + f(thick, entry, res, target)
R²=0.605 · MAE ±5.2°C · 30,655 slab records
Primary driver: recipe target (r=+0.669). Z3 zone: +0.08°C/°C. Coffin load: −8.2°C penalty
M3
Flue Gas Temperature Model
FGT = 590.9 + Σ(FGT_Zi × actual_i) + f(O₂, Pressure, Damper, AFR)
R²=0.696 · MAE ±15.9°C · 3,955 hours
Key lever: AFR +1 → FGT −18.8°C. Damper r=+0.72. Validates FGT improvement potential
ZONE WEIGHTED AVERAGE TEMPERATURE: T_wt = Σ(zone_fuel_i × zone_actual_i) / Σ(zone_fuel_i) — weights preheat/heating zones by actual energy delivered

## Slide 3
5-SCHEDULE PORTFOLIO — SUMMARY COMPARISON
Schedule | Date / Shift | Slabs | On-Target | Mean Deviation | Curr Wt Avg | Curr Fuel | Saving | Status
20251783 | 03 Oct 2025 Afternoon | 15 | 14/15 | +5.9°C | 1265.8°C | 40,985 | 3,326 (8.1%) | GOOD
20251904 | 18 Oct 2025 Morning | 11 | 9/11 | +1.4°C | 1221.7°C | 25,805 | 1,697 (6.6%) | GOOD
20252023 | 06 Nov 2025 Night | 14 | 8/14 | -5.1°C | 1210.0°C | 21,785 | 824 (3.8%) | UNDER-FIRED
20252089 | 16 Nov 2025 Afternoon | 13 | 13/13 | +9.8°C | 1227.3°C | 27,006 | 3,389 (12.5%) | OVER-FIRED
20252354 | 24 Dec 2025 Morning | 6 | 6/6 | +5.6°C | 1191.3°C | 4,518 | 354 (7.8%) | OVER-FIRED
Chart: Fuel (Nm³/hr) — Current vs Saving Potential
| 1783 | 1904 | 2023 | 2089 | 2354
Current Fuel | 40985 | 25805 | 21785 | 27006 | 4518
Saving Potential | 3326 | 1697 | 824 | 3389 | 354
Chart: Mean FCE Deviation per Schedule (°C)
| 1783 | 1904 | 2023 | 2089 | 2354
Mean FCE Deviation (°C) | 5.9 | 1.4 | -5.1 | 9.8 | 5.6

## Slide 4
SCHEDULE 20251783 | 03 Oct 2025 15:42 (Afternoon Shift)
ON-TARGET
Grade mix: Multi-grade (ANCRMB6/ANIFS01/ANTRN series) | Thickness: 217–230 mm
# | Grade | Thk | Entry°C | Target°C | Actual FCE | Dev | Status
1 | ANCRMB6 | 230 | 37⚠ | 1230.0 | 1231.7 | +1.5° | ✓ OK
2 | ANIFS01 | 217 | 44⚠ | 1220.0 | 1238.6 | +18.4° | ✓ OK
3 | ANCRP09 | 217 | 432 | 1230.0 | 1243.4 | +13.3° | ✓ OK
4 | ANEDD02 | 217 | 53⚠ | 1230.0 | 1238.4 | +8.3° | ✓ OK
5 | ANTRN51 | 217 | 35⚠ | 1230.0 | 1235.5 | +5.3° | ✓ OK
6 | ANGEN02 | 230 | 43⚠ | 1240.0 | 1228.9 | -11.2° | ✕ FAIL
7 | ANIFS01 | 217 | 38⚠ | 1230.0 | 1236.0 | +5.8° | ✓ OK
8 | ANDRWB2 | 217 | 53⚠ | 1230.0 | 1236.8 | +6.7° | ✓ OK
9 | ANTRN65 | 217 | 47⚠ | 1230.0 | 1232.8 | +2.7° | ✓ OK
10 | ANTRN65 | 217 | 44⚠ | 1220.0 | 1227.3 | +7.2° | ✓ OK
11 | ANTRN33 | 217 | 49⚠ | 1220.0 | 1223.6 | +3.4° | ✓ OK
12 | ANTRK65 | 217 | 46⚠ | 1220.0 | 1223.1 | +3.0° | ✓ OK
13 | ANTRK65 | 217 | 46⚠ | 1220.0 | 1227.0 | +6.8° | ✓ OK
14 | ANTRK65 | 217 | 50⚠ | 1220.0 | 1228.5 | +8.4° | ✓ OK
15 | ANTRN04 | 217 | 67⚠ | 1220.0 | 1229.8 | +9.6° | ✓ OK
ZONE TEMPERATURE — CURRENT vs OPTIMAL
−30
1242
Z1
PRE
−35
1238
Z2
PRE
−20
1321
Z3
HEAT
−15
1320
Z4
HEAT
−8
1245
Z5
SOAK
−8
1244
Z6
SOAK
−8
1247
Z7
SOAK
−8
1244
Z8
DISC
Current actual temp
Optimal SP → actual
Fuel Weight Avg
1265.8°C
→ 1238.4°C
Optimised
Total Fuel
40,985
→ 37,659
Optimised
FCE On-Target
14/15
→ 15/15
Optimised
Mean FCE Dev
+5.9°C
→ ±2°C
Optimised
🔍 14/15 slabs OVER-fired (avg +5.9°C). Z1/Z2 setpoints 1264°C vs optimal 1229–1234°C. ANGEN02 slab failed (−11.2°C) due to higher target 1240°C while furnace cooling during shift.
▶ Reduce Z1/Z2 SP by 30–35°C. Reduce Z3/Z4 by 15–20°C. Compensate ANGEN02 slabs by raising Z7/Z8 SP.

## Slide 5
SCHEDULE 20251904 | 18 Oct 2025 07:42 (Morning Shift)
ON-TARGET
Grade mix: ANCRMB6 / ANEDD04 / ANGEN15 / ANLNP41 / ANWTPT3 | Thickness: 210–230 mm
# | Grade | Thk | Entry°C | Target°C | Actual FCE | Dev | Status
1 | ANCRMB6 | 230 | 53⚠ | 1230.0 | 1227.5 | -2.7° | ✓ OK
2 | ANEDD04 | 217 | 193 | 1230.0 | 1234.0 | +3.9° | ✓ OK
3 | ANGEN15 | 210 | 82⚠ | 1230.0 | 1240.0 | +9.8° | ✓ OK
4 | ANGEN15 | 210 | 114⚠ | 1230.0 | 1244.5 | +14.4° | ✓ OK
5 | ANLNP41 | 217 | 189 | 1245.0 | 1247.0 | +1.9° | ✓ OK
6 | ANLNP41 | 217 | 190 | 1245.0 | 1248.9 | +3.8° | ✓ OK
7 | ANLNP41 | 217 | 216 | 1245.0 | 1248.1 | +2.9° | ✓ OK
8 | ANLNP41 | 217 | 219 | 1245.0 | 1244.8 | -0.3° | ✓ OK
9 | ANLNP41 | 217 | 64⚠ | 1245.0 | 1235.6 | -9.5° | ✕ FAIL
10 | ANLNP41 | 217 | 85⚠ | 1245.0 | 1234.8 | -10.3° | ✕ FAIL
11 | ANWTPT3 | 217 | 61⚠ | 1230.0 | 1231.6 | +1.5° | ✓ OK
ZONE TEMPERATURE — CURRENT vs OPTIMAL
−20
1174
Z1
PRE
−25
1154
Z2
PRE
−15
1320
Z3
HEAT
−10
1319
Z4
HEAT
−5
1238
Z5
SOAK
−5
1240
Z6
SOAK
−5
1222
Z7
SOAK
−5
1221
Z8
DISC
Current actual temp
Optimal SP → actual
Fuel Weight Avg
1221.7°C
→ 1203.5°C
Optimised
Total Fuel
25,805
→ 24,108
Optimised
FCE On-Target
9/11
→ 11/11
Optimised
Mean FCE Dev
+1.4°C
→ ±2°C
Optimised
🔍 2 ANLNP41 slabs failed (entry temp 64–85°C, target 1245°C). Cold-entry slabs need zone compensation — Z7/Z8 SP insufficient at 1235°C. O₂ high at 6.8% → excess air waste.
▶ Raise Z7/Z8 SP to 1245°C for ANLNP41 cold-entry slabs. Reduce AFR to 11.5, lower O₂ to ≤5% to save combustion air. Reduce Z1/Z2 SP 20–25°C.

## Slide 6
SCHEDULE 20252023 | 06 Nov 2025 21:25 (Night Shift)
UNDER-FIRED — QUALITY RISK
Grade mix: ANCRMB2 / ANTRNT5 / ANGEN02 / ANSCG27 / ANCRMB6 | Thickness: 217–230 mm
# | Grade | Thk | Entry°C | Target°C | Actual FCE | Dev | Status
1 | ANCRMB2 | 230 | 42⚠ | 1230.0 | 1226.3 | -3.9° | △
2 | ANTRNT5 | 217 | 81⚠ | 1220.0 | 1226.1 | +5.9° | ✓ OK
3 | ANTRNT5 | 217 | 187 | 1220.0 | 1225.0 | +4.8° | ✓ OK
4 | ANTRNT5 | 217 | 183 | 1220.0 | 1226.1 | +6.0° | ✓ OK
5 | ANTRNT5 | 217 | 180 | 1220.0 | 1228.6 | +8.5° | ✓ OK
6 | ANTRNT5 | 217 | 96⚠ | 1220.0 | 1230.7 | +10.6° | ✓ OK
7 | ANGEN02 | 220 | 80⚠ | 1230.0 | 1231.0 | +0.8° | ✓ OK
8 | ANGENT6 | 217 | 54⚠ | 1230.0 | 1232.8 | +2.6° | ✓ OK
9 | ANSCG27 | 217 | 80⚠ | 1230.0 | 1209.8 | -20.4° | ✕ FAIL
10 | ANSCG27 | 217 | 86⚠ | 1230.0 | 1207.0 | -23.2° | ✕ FAIL
11 | ANCRMB2 | 230 | 71⚠ | 1230.0 | 1204.6 | -25.6° | ✕ FAIL
12 | ANCRMB2 | 230 | 49⚠ | 1230.0 | 1208.5 | -21.7° | ✕ FAIL
13 | ANCRMB2 | 230 | 44⚠ | 1230.0 | 1214.4 | -15.8° | ✕ FAIL
14 | ANCRMB6 | 220 | 60⚠ | 1220.0 | 1220.2 | 0.0° | ✓ OK
ZONE TEMPERATURE — CURRENT vs OPTIMAL
−15
1213
Z1
PRE
−15
1187
Z2
PRE
−5
1259
Z3
HEAT
−5
1236
Z4
HEAT
1234
Z5
SOAK
1230
Z6
SOAK
1237
Z7
SOAK
1216
Z8
DISC
Current actual temp
Optimal SP → actual
Fuel Weight Avg
1210.0°C
→ 1198.2°C
Optimised
Total Fuel
21,785
→ 20,961
Optimised
FCE On-Target
8/14
→ 13/14
Optimised
Mean FCE Dev
-5.1°C
→ ±2°C
Optimised
🔍 WORST SCHEDULE: 5 slabs SEVERELY under-fired (−16 to −26°C). ANSCG27 and thick ANCRMB2 (230mm) slabs failed catastrophically. Z3/Z4 SPs were too low (1259/1236°C). Residence time very long (71 min heating) but zone temp was still insufficient.
▶ RAISE Z3 SP to minimum 1290°C for thick 230mm slabs. Reduce residence time in preheat (160 min excess). Grade mix change needed — 230mm slabs require separate setpoints.

## Slide 7
SCHEDULE 20252089 | 16 Nov 2025 13:18 (Afternoon Shift)
OVER-FIRED
Grade mix: ANCRMB6 / ANEDG02 / ANEDD02 / ANTRW04 / ANTRS65 | Thickness: 210–220 mm
# | Grade | Thk | Entry°C | Target°C | Actual FCE | Dev | Status
1 | ANCRMB6 | 218 | 38⚠ | 1230.0 | 1248.6 | +18.5° | ✓ OK
2 | ANEDG02 | 217 | 452 | 1230.0 | 1246.0 | +15.9° | ✓ OK
3 | ANEDD02 | 217 | 148 | 1220.0 | 1240.9 | +20.8° | ✓ OK
4 | ANEDD02 | 217 | 161 | 1220.0 | 1237.4 | +17.2° | ✓ OK
5 | ANEDD02 | 217 | 161 | 1220.0 | 1233.7 | +13.6° | ✓ OK
6 | ANCRMB6 | 220 | 131⚠ | 1220.0 | 1231.6 | +11.4° | ✓ OK
7 | ANCRMB6 | 220 | 57⚠ | 1220.0 | 1228.6 | +8.4° | ✓ OK
8 | ANCRMB6 | 220 | 59⚠ | 1220.0 | 1226.0 | +5.8° | ✓ OK
9 | ANTRW04 | 217 | 111⚠ | 1220.0 | 1225.5 | +5.3° | ✓ OK
10 | ANTRN37 | 210 | 48⚠ | 1220.0 | 1224.6 | +4.5° | ✓ OK
11 | ANTRS65 | 217 | 111⚠ | 1220.0 | 1221.3 | +1.2° | ✓ OK
12 | ANTRS65 | 217 | 108⚠ | 1220.0 | 1221.0 | +0.9° | ✓ OK
13 | ANTRS65 | 217 | 77⚠ | 1220.0 | 1224.2 | +4.0° | ✓ OK
ZONE TEMPERATURE — CURRENT vs OPTIMAL
−40
1227
Z1
PRE
−45
1206
Z2
PRE
−30
1271
Z3
HEAT
−20
1254
Z4
HEAT
−12
1242
Z5
SOAK
−12
1244
Z6
SOAK
−12
1238
Z7
SOAK
−12
1237
Z8
DISC
Current actual temp
Optimal SP → actual
Fuel Weight Avg
1227.3°C
→ 1189.7°C
Optimised
Total Fuel
27,006
→ 23,617
Optimised
FCE On-Target
13/13
→ 13/13
Optimised
Mean FCE Dev
+9.8°C
→ ±2°C
Optimised
🔍 BEST QUALITY, WORST ENERGY: 13/13 on-target but mean deviation +9.8°C — furnace massively over-fired. Pre-heating residence 239 min (almost 4 hours!). Z1/Z2 SP 1249/1232°C can be reduced by 40–45°C. Largest single saving opportunity.
▶ Reduce Z1/Z2 SP by 40–45°C, Z3/Z4 by 20–30°C. Review and reduce preheat residence time from 239 min to ≤140 min. This schedule has the highest saving potential: 3,389 Nm³/hr.

## Slide 8
SCHEDULE 20252354 | 24 Dec 2025 08:17 (Morning Shift)
OVER-FIRED
Grade mix: ANCRMB2 / ANTRG55 / ANTRG13 | Thickness: 217 mm
# | Grade | Thk | Entry°C | Target°C | Actual FCE | Dev | Status
1 | ANCRMB2 | 217 | 211 | 1230.0 | 1236.1 | +5.9° | ✓ OK
2 | ANTRG55 | 217 | 64⚠ | 1220.0 | 1233.1 | +13.0° | ✓ OK
3 | ANTRG55 | 217 | 64⚠ | 1220.0 | 1229.3 | +9.1° | ✓ OK
4 | ANTRG55 | 217 | 51⚠ | 1220.0 | 1226.3 | +6.2° | ✓ OK
5 | ANTRG13 | 217 | 121⚠ | 1220.0 | 1222.5 | +2.3° | ✓ OK
6 | ANTRG13 | 217 | 60⚠ | 1220.0 | 1217.2 | -2.9° | ✓ OK
ZONE TEMPERATURE — CURRENT vs OPTIMAL
−30
1151
Z1
PRE
−35
1062
Z2
PRE
−20
1315
Z3
HEAT
−15
1315
Z4
HEAT
−8
1237
Z5
SOAK
−8
1215
Z6
SOAK
−8
1237
Z7
SOAK
−8
1215
Z8
DISC
Current actual temp
Optimal SP → actual
Fuel Weight Avg
1191.3°C
→ 1172.0°C
Optimised
Total Fuel
4,518
→ 4,164
Optimised
FCE On-Target
6/6
→ 6/6
Optimised
Mean FCE Dev
+5.6°C
→ ±2°C
Optimised
🔍 Small 6-slab schedule, all on-target. AFR 15.02 (very lean — good combustion). Low furnace load: Z1/Z2 actual only 1151/1062°C but setpoints 1173/1088°C. ANTRG13 last slab borderline (−2.9°C) — residual risk if cooling trend continues.
▶ Reduce Z3/Z4 SP by 15–20°C. Maintain AFR at 14–15 (already efficient). Monitor last-slab temperature drop — schedule more slabs or reduce gaps between schedules.

## Slide 9
OPTIMISATION SEQUENCE — HOW THE MODEL ACTS
1
DIAGNOSE
T+0 min
Read Schedule + Actual Zone Conditions
• Match slab discharge timestamps to hourly process records
• Compute fuel-weighted zone avg temperature per schedule
• Identify over/under-firing per slab (FCE vs target recipe)
2
PREDICT
T+0.5 min
Run FCE Dropout Prediction (M2)
• Predict FCE for every slab using zone actuals + slab parameters
• Flag slabs where predicted FCE < target − 3°C (at risk)
• Identify cold-entry slabs (entry < 140°C) needing compensation
3
OPTIMISE
T+1 min
Advisory Engine — Minimise Fuel
• Reduce Z1/Z2 SP first (largest fuel contributors: 43% + 23%)
• Step down Z3/Z4 SP by smaller amounts (protect FCE quality)
• Verify all predicted FCE ≥ target − 3°C before confirming
4
COMPENSATE
T+1 min
Zone Compensation for Cold Slabs
• Cold slabs (entry < 140°C) flagged: FCE deficit = 0.002328 × (167 − entry)
• Z3 best compensator: +1°C SP recovers 0.08°C FCE
• Z7/Z8 secondary: model specifies exact SP increase needed
5
VALIDATE
T+2 min
FGT Check (M3) + Fuel Saving Confirmation
• Predict new chimney FGT at optimised SP — must remain < 460°C
• Confirm total fuel saving: Σ(slope_i × ΔSP_i) per zone
• Output: SP recommendations + saving Nm³/hr + FGT status
6
APPLY
T+3 min
Operator Applies — Shift Report Generated
• One-click Apply Optimal — all 8 SPs updated simultaneously
• Shift report: KPI comparison, zone grid, compensation status
• Estimated saving at ₹18/Nm³: quantified per schedule

## Slide 10
AGGREGATE RESULTS — CURRENT STATE vs TARGET STATE
⚡
120,099
Nm³/hr total current fuel (5 schedules)
✓
9,590
Nm³/hr saving potential identified
↓
8.0%
average fuel reduction across schedules
◎
50/59
slabs on-target current state
⚠
8
slabs failed FCE target (below −8°C)
Schedule | Date | n | Curr Fuel | → Opt Fuel | Saving | Save% | Curr Wt T | → Opt Wt T | FCE Dev | On-Tgt
1783 | 03 Oct | 15 | 40,985 | 37,659 | 3,326 | 8.1% | 1265.8° | 1238.4° | +5.9° | 14/15
1904 | 18 Oct | 11 | 25,805 | 24,108 | 1,697 | 6.6% | 1221.7° | 1203.5° | +1.4° | 9/11
2023 | 06 Nov | 14 | 21,785 | 20,961 | 824 | 3.8% | 1210.0° | 1198.2° | -5.1° | 8/14
2089 | 16 Nov | 13 | 27,006 | 23,617 | 3,389 | 12.5% | 1227.3° | 1189.7° | +9.8° | 13/13
2354 | 24 Dec | 6 | 4,518 | 4,164 | 354 | 7.8% | 1191.3° | 1172.0° | +5.6° | 6/6
TOTAL | — | 59 | 120,099 | 110,509 | 9,590 | 8.0% | — | — | — | 50/59
🔥 Over-firing
Sched 1783 (+5.9°C) and 2089 (+9.8°C): Operator SPs set 30–45°C above model optimum. Z1/Z2 primary culprit.
❄ Under-heating
Sched 2023 (−5.1°C): 5 slabs severely failed. Z3/Z4 SPs too low for thick 230mm grades + grade mix without SP segmentation.
⚠ Cold slab entry
Sched 1904: ANLNP41 with 64–85°C entry temp failed −9.5 to −10.3°C. No zone compensation applied.

## Slide 11
CONCLUSIONS & RECOMMENDATIONS
C1
FINDING
Over-firing is the dominant issue
3 of 5 schedules over-fired: avg excess +7.1°C. All on-target but burning 8–12.5% more fuel than needed. Largest opportunity: Schedule 2089 — 3,389 Nm³/hr saving with zero quality risk.
C2
FINDING
Grade-mix without SP segmentation causes failures
Schedule 2023: thick 230mm ANCRMB2/ANSCG27 slabs failed badly (−16 to −26°C) while thinner slabs were fine on same SP. Model must recommend different Z3/Z4 SPs by grade group.
C3
FINDING
Cold-entry compensation not being applied
Schedule 1904: ANLNP41 slabs with 64–85°C entry temp failed despite adequate zone temps. Downstream zone compensation (Z7/Z8 +15–20°C) would have fully recovered FCE.
R1
RECOMMENDATION
Deploy advisory model for every shift
Run optimiser at shift start: input 8-slab queue + zone temps → receive optimal SP within 2 min. Expected saving: 3,000–5,000 Nm³/hr per schedule · ~₹54k–₹90k per shift.
R2
RECOMMENDATION
Implement fuel-weighted zone avg as daily KPI
Current practice ignores fuel distribution. Fuel-weighted avg temp shows true thermal delivery. Target: maintain <1,240°C weighted avg. Schedule 2089 was 1,227°C — achievable at 1,190°C.
Source: 30,731 slab records + 4,344 hrs process data · Hazira RHF-1 · Aug–Dec 2025 · Model: FCE R²=0.605 · FGT R²=0.696