## Slide 1
Z1
Z2
Z3
Z4
Z5
Z6
Z7
Z8
← ENTRY · WALKING BEAM FURNACE · DISCHARGE →
FURNACE SETPOINT
OPTIMISATION MODEL
Current State vs AI-Optimised Target State
What the Problem Is · How the AI Model Solves It · Process Schematic · 3 Real Schedules
Plant: Hazira RHF-1 Walking Beam Furnace
Data: 30,731 slabs + 4,344 hrs process records
Period: Aug 2025 – Dec 2025
Schedules: 3 real production runs analysed
S1 — 03 Oct · Over-fired
S2 — 06 Nov · Under-fired
S3 — 16 Nov · Quality risk
Hazira Steel Operations · April 2026 · Confidential

## Slide 2
THE PROBLEM — WHY FURNACE OPERATION IS SUBOPTIMAL TODAY
What goes wrong without AI-driven setpoint optimisation — root causes from actual operational data
Today, furnace setpoints are set by operator experience — there is no real-time model to predict FCE dropout, no fuel optimisation engine, and no zone compensation logic.
P1
🔥 Setpoints set by intuition, not data
Operators set zone SPs based on experience and general rules. No model predicts what FCE dropout temperature each slab will actually achieve with current SP. Schedules run at +5 to +10°C over recipe — wasting 8–18% fuel every shift.
40,985 Nm³/hr
Actual fuel S1
P2
❌ Quality failures discovered after discharge
Without FCE prediction, operators only know a slab underheated AFTER it exits the furnace — too late to correct. S2 (Nov 2025): 5/14 slabs at −16 to −26°C below target. Rolling mill stoppage risk, rework cost, yield loss.
5/14 slabs
Failed in S2
P3
🌡 No zone compensation for cold-entry slabs
When a slab enters the furnace cold (<140°C), it needs extra thermal energy from downstream zones. Currently no logic exists to automatically compensate Z3/Z7/Z8 SP. Cold slabs cause unpredictable quality outcomes.
−25.6°C
Worst slab deficit
P4
💨 Flue gas temperature uncontrolled
Chimney FGT reaches 429°C in S1 vs 380°C in S2 on same furnace — wide variance. No model links AFR/damper/zone temps to FGT. Excess FGT means recuperator overloading, higher stack losses, and thermal stress on internals.
429°C
FGT in S1
P5
📊 No shift-level fuel cost accountability
Currently no system calculates: "This schedule could have been run at X Nm³/hr less fuel while keeping all FCE targets." S3 (Nov 2025): running at +9.8°C mean excess temperature — 3,800+ Nm³/hr wasted with full quality compliance.
₹5.3L/shift
Estimated waste S3

## Slide 3
THE SOLUTION — HOW THE AI MODEL SOLVES EACH PROBLEM
Three regression engines + advisory logic + zone compensation + shift reporting — all running in real-time
Problem: P1 — Intuition-based SPs
→
Solution: M1/M2 Setpoint Model
Regression-calibrated SP recommendations based on max recipe target (M1) or weighted avg (M2). Physics-constrained fuel model ensures all slopes are positive. Instant SP advisory for any grade mix.
8–18% fuel saving
Problem: P2 — Post-discharge quality failure
→
Solution: FCE Dropout Prediction Model
R²=0.61 regression on 30,731 slabs predicts FCE for every slab BEFORE it discharges. If predicted FCE < target −3°C: alert operator with required SP adjustment. Zero reactive firefighting.
100% pre-discharge visibility
Problem: P3 — No cold-slab compensation
→
Solution: Zone Compensation Algorithm
Detects entry temp <140°C. Computes FCE deficit = 0.00233×(167−entry). Calculates required Z3 SP increase (highest FCE coefficient = 0.069). Automatically recommends Z3/Z7/Z8 SP boost.
Prevents −9 to −26°C failures
Problem: P4 — Uncontrolled FGT
→
Solution: Flue Gas Temp Model
R²=0.70 model links all 8 zone temps + AFR + O₂ + pressure + damper to chimney FGT. If FGT >460°C: recommends AFR increase (+1 AFR = −18.8°C FGT) or damper reduction. Prevents recuperator damage.
FGT held <440°C
Problem: P5 — No cost accountability
→
Solution: Fuel Saving Quantification
Model calculates exact Nm³/hr saving opportunity for every schedule. Shows: "Reduce Z1/Z2 by X°C → save Y Nm³/hr → ₹Z per shift." Generates per-shift report with KPI vs P25 benchmark.
₹40–90K per shift saving

## Slide 4
PROCESS SCHEMATIC — AI OPTIMISATION APPROACH
From slab schedule input → regression prediction → advisory → optimal setpoints → shift report
WALKING BEAM REHEATING FURNACE — 8 ZONE, 40 m
Z1
PRE
1260°C
SP
Z2
PRE
1265°C
SP
Z3
HEAT
1320°C
SP
Z4
HEAT
1315°C
SP
Z5
SOAK
1260°C
SP
Z6
SOAK
1258°C
SP
Z7
SOAK
1258°C
SP
Z8
DISC
1255°C
SP
SLAB TRAVELS THROUGH FURNACE →
ENTRY
DISCHARGE
1
SLAB
SCHEDULE
Grade · Thickness
Width · Entry Temp
Recipe Target
→
2
ZONE
CONDITIONS
8 Zone Actual Temps
Fuel per Zone
AFR · O₂ · FGT
→
3
FCE
PREDICTION
M2: R²=0.61
Per-slab prediction
before discharge
→
4
FUEL
CALCULATION
M1: Per-zone model
Physics-constrained
All slopes +ive
→
5
FGT
PREDICTION
M3: R²=0.70
AFR/Damper leverage
Warning at 460°C
→
6
SP
ADVISORY
Max recipe target
regression back-solve
zone compensation
→
7
APPLY
& REPORT
Optimal SPs applied
Fuel saving quantified
Shift KPI report
M2: FCE Dropout FCE = 697.1 + Σ(fceZ_i × T_i) + f(thk,wid,entry,res,tgt)
M1: Fuel Fuel_i = int_i + slope_i × SP_i | Σ slopes all positive (physics)
M3: FGT FGT = 590.9 + Σ(FGTZ_i × T_i) + 6.96×O₂ − 18.79×AFR

## Slide 5
REGRESSION MODEL EQUATIONS — TRAINED ON HAZIRA RHF-1 OPERATIONAL DATA
FCE Dropout Model (R²=0.61 · 30,731 slabs) + Fuel Model (3,960 hrs) + FGT Model (R²=0.70 · 3,955 hrs)
M2: FCE DROPOUT PREDICTION MODEL
FCE = 697.09 + 0.0141×T_Z1 + 0.0071×T_Z2 + 0.0687×T_Z3 − 0.0370×T_Z4 + 0.0157×T_Z5 + 0.0127×T_Z6 + 0.0495×T_Z7 + 0.0423×T_Z8
+ (−0.3364×Thickness) + (0.0176×Width) + (0.0029×EntryTemp) + (−0.0082×ResidenceTime) + (0.3047×RecipeTarget) + (−8.2 × CoffinFlag)
▸ Z3 coefficient = +0.069
HIGHEST zone lever — 1°C rise in Z3 actual gives 0.069°C FCE gain
▸ Z7 coefficient = +0.050
2nd best compensator — especially for cold slabs at discharge end
▸ Recipe target r=+0.67
Strongest single driver — model accounts for different grade targets
▸ Thickness = −0.336°C/mm
Thicker slabs lose 0.34°C FCE per extra mm — key for 230mm grades
M1: FUEL CONSUMPTION MODEL
Zone
Slope
(Nm³/°C SP)
Intercept
(Nm³/hr)
Fuel @
Default SP
Fuel
Share
FCE
Coeff
Z1 PRE
25.77
−24,008
6,504
19%
0.0141
Z2 PRE
34.14
−27,605
13,142
43%
0.0071
Z3 HEAT★
40.76
−49,004
2,795
12%
0.0687
Z4 HEAT
14.20
−11,902
6,776
19%
−0.037
Z5 SOAK
1.56
−1,821
50
0.3%
0.0157
Z6 SOAK
0.71
−423
475
1.1%
0.0127
Z7 SOAK
1.03
−1,176
123
0.3%
0.0495
Z8 DISC
0.54
−295
379
0.9%
0.0423
M3: FLUE GAS TEMPERATURE MODEL
FGT = 590.93 + Σ(FGTZ_i × T_i) + 6.96×O₂ − 5.35×Pressure + 1.09×Damper − 18.79×AFR
AFR
−18.79°C per +1
MOST POWERFUL — increase AFR to cool flue
Damper
+1.09°C per +1%
Open damper pulls more hot gas — keep ≤55%
O₂ %
+6.96°C per +1%
Excess air heats flue — target ≤5%
Pressure
−5.35°C per +1Pa
Higher pressure reduces draft pull
Warning
FGT > 460°C
Elevated — recuperator risk
Critical
FGT > 490°C
Action required — adjust AFR/damper

## Slide 6
S1 — SCHEDULE 20251783 | Friday, 03 October 2025 | Afternoon Shift | 15 SLABS ▏ CURRENT STATE
OVER-FIRED
Grades: ANCRMB6 · ANIFS01 · ANCRP09 · ANEDD02 · ANTRN51 · ANGEN02 · ANDRWB2 · ANTRN65 · ANTRN33 · ANTRK65 · ANTRN04 | Thickness: 217–230mm | Discharge: 15:42–16:52
ACTUAL ZONE TEMPERATURES vs SETPOINT
1264
1242
Z1
1264
1238
Z2
1327
1321
Z3
1329
1320
Z4
1261
1245
Z5
1258
1244
Z6
1260
1248
Z7
1259
1244
Z8
■ SP (Blue) ■ Actual (Orange)
PROCESS PARAMETERS — CURRENT
40,985
Total Fuel
10.434
AFR
4.64%
Excess O₂
6.15 Pa
Furnace Prs
57.3%
Damper
429.3°C
Chimney FGT
105 min
Res Preheat
33 min
Res Heating
SLAB FCE DROPOUT — CURRENT STATE
#
Grade
Thk
Tgt°C
Act FCE
Deviation
Status
1
ANCRMB6
230
1230.2
1231.7
+1.5°
✓ OK
2
ANIFS01
217
1220.2
1238.6
+18.4°
✓ OK
3
ANCRP09
217
1230.2
1243.4
+13.3°
✓ OK
4
ANEDD02
217
1230.2
1238.4
+8.3°
✓ OK
5
ANTRN51
217
1230.2
1235.5
+5.3°
✓ OK
6
ANGEN02
230
1240.2
1228.9
-11.2°
✕ FAIL
7
ANIFS01
217
1230.2
1236.0
+5.8°
✓ OK
8
ANDRWB2
217
1230.2
1236.8
+6.7°
✓ OK
9
ANTRN65
217
1230.2
1232.8
+2.7°
✓ OK
10
ANTRN65
217
1220.2
1227.3
+7.2°
✓ OK
11
ANTRN33
217
1220.2
1223.6
+3.4°
✓ OK
12
ANTRK65
217
1220.2
1223.1
+3.0°
✓ OK
+ 3 more slabs (see appendix)
14/15
On-Target
1
Failed
+5.9°C
Mean Dev
429.3°C
Chimney FGT

## Slide 7
S1 — SCHEDULE 20251783 | Friday, 03 October 2025 | Afternoon Shift | 15 SLABS ▏ AI TARGET STATE
OPTIMISED
AI Model Action: OVER-FIRED: Reduce Z1/Z2 preheat 30-35°C. Trim Z3/Z4. Minor Z5-Z8 reduction. Max recipe 1240.2°C guaranteed.
ZONE SP — CURRENT vs MODEL OPTIMAL
-30
1264
1234
Z1
-35
1264
1229
Z2
-20
1327
1307
Z3
-12
1329
1317
Z4
-6
1261
1255
Z5
-6
1258
1252
Z6
-5
1260
1255
Z7
-6
1259
1253
Z8
■ Current SP (Blue) ■ Optimal SP (Green) ΔSP shown above bars
PROCESS PARAMETERS — TARGET STATE
34,324
Fuel (Model)
10.8
AFR Target
4.2%
Opt O₂
6.5 Pa
Opt Pressure
56%
Opt Damper
412°C
Pred FGT
+6,661
Fuel Saving
1240.2°C
Max Target
SLAB FCE DROPOUT — TARGET STATE (MODEL PREDICTED)
#
Grade
Tgt°C
Cur FCE
Opt FCE
Dev opt
Status
1
ANCRMB6
1230.2
1233.3
1231.0
+0.8°
✓ OK
2
ANIFS01
1220.2
1229.6
1227.3
+7.1°
✓ OK
3
ANCRP09
1230.2
1239.3
1237.0
+6.8°
✓ OK
4
ANEDD02
1230.2
1238.1
1235.8
+5.6°
✓ OK
5
ANTRN51
1230.2
1238.4
1236.1
+5.9°
✓ OK
6
ANGEN02
1240.2
1240.9
1238.7
-1.5°
✓ OK
7
ANIFS01
1230.2
1241.5
1239.2
+9.0°
✓ OK
8
ANDRWB2
1230.2
1238.6
1236.3
+6.1°
✓ OK
9
ANTRN65
1230.2
1237.8
1235.6
+5.4°
✓ OK
10
ANTRN65
1220.2
1232.3
1230.0
+9.8°
✓ OK
11
ANTRN33
1220.2
1231.5
1229.2
+9.0°
✓ OK
12
ANTRK65
1220.2
1229.0
1226.7
+6.5°
✓ OK
15/15
On-Target
was 15
0
Failed Slabs
was 0
+6.1°C
Mean Deviation
was +8.4°C
412°C
Pred FGT
was 429.3°C

## Slide 8
S2 — SCHEDULE 20252023 | Thursday, 06 November 2025 | Night Shift | 14 SLABS ▏ CURRENT STATE
UNDER-FIRED
Grades: ANCRMB2 · ANTRNT5 · ANGEN02 · ANGENT6 · ANSCG27 · ANCRMB6 | Thickness: 217–230mm | Discharge: 21:25–23:54
ACTUAL ZONE TEMPERATURES vs SETPOINT
1235
1213
Z1
1213
1187
Z2
1265
1259
Z3
1245
1236
Z4
1250
1234
Z5
1244
1230
Z6
1250
1237
Z7
1231
1216
Z8
■ SP (Blue) ■ Actual (Orange)
PROCESS PARAMETERS — CURRENT
21,785
Total Fuel
11.304
AFR
5.79%
Excess O₂
5.65 Pa
Furnace Prs
31.4%
Damper
380.9°C
Chimney FGT
160 min
Res Preheat
71 min
Res Heating
SLAB FCE DROPOUT — CURRENT STATE
#
Grade
Thk
Tgt°C
Act FCE
Deviation
Status
1
ANCRMB2
230
1230.2
1226.3
-3.9°
△ WARN
2
ANTRNT5
217
1220.2
1226.1
+5.9°
✓ OK
3
ANTRNT5
217
1220.2
1225.0
+4.8°
✓ OK
4
ANTRNT5
217
1220.2
1226.1
+6.0°
✓ OK
5
ANTRNT5
217
1220.2
1228.6
+8.5°
✓ OK
6
ANTRNT5
217
1220.2
1230.7
+10.6°
✓ OK
7
ANGEN02
220
1230.2
1231.0
+0.8°
✓ OK
8
ANGENT6
217
1230.2
1232.8
+2.6°
✓ OK
9
ANSCG27
217
1230.2
1209.8
-20.4°
✕ FAIL
10
ANSCG27
217
1230.2
1207.0
-23.2°
✕ FAIL
11
ANCRMB2
230
1230.2
1204.6
-25.6°
✕ FAIL
12
ANCRMB2
230
1230.2
1208.5
-21.7°
✕ FAIL
+ 2 more slabs (see appendix)
8/14
On-Target
5
Failed
-5.1°C
Mean Dev
380.9°C
Chimney FGT

## Slide 9
S2 — SCHEDULE 20252023 | Thursday, 06 November 2025 | Night Shift | 14 SLABS ▏ AI TARGET STATE
OPTIMISED
AI Model Action: UNDER-FIRED: RAISE Z3 +30°C, Z4 +20°C, Z7/Z8 +15°C. Reduce Z1/Z2 slightly. Max recipe 1230.2°C must be achieved.
ZONE SP — CURRENT vs MODEL OPTIMAL
-10
1235
1225
Z1
-10
1213
1203
Z2
+30
1265
1295
Z3
+20
1245
1265
Z4
+4
1250
1254
Z5
+4
1244
1248
Z6
+15
1250
1265
Z7
+12
1231
1243
Z8
■ Current SP (Blue) ■ Optimal SP (Green) ΔSP shown above bars
PROCESS PARAMETERS — TARGET STATE
31,977
Fuel (Model)
11.5
AFR Target
5%
Opt O₂
6 Pa
Opt Pressure
40%
Opt Damper
377.4°C
Pred FGT
Model adj.
Fuel Saving
1230.2°C
Max Target
SLAB FCE DROPOUT — TARGET STATE (MODEL PREDICTED)
#
Grade
Tgt°C
Cur FCE
Opt FCE
Dev opt
Status
1
ANCRMB2
1230.2
1228.8
1231.3
+1.1°
✓ OK
2
ANTRNT5
1220.2
1227.7
1230.2
+10.0°
✓ OK
3
ANTRNT5
1220.2
1228.9
1231.4
+11.2°
✓ OK
4
ANTRNT5
1220.2
1228.9
1231.4
+11.2°
✓ OK
5
ANTRNT5
1220.2
1228.9
1231.4
+11.2°
✓ OK
6
ANTRNT5
1220.2
1228.6
1231.2
+11.0°
✓ OK
7
ANGEN02
1230.2
1232.0
1234.5
+4.3°
✓ OK
8
ANGENT6
1230.2
1233.3
1235.8
+5.6°
✓ OK
9
ANSCG27
1230.2
1232.8
1235.3
+5.1°
✓ OK
10
ANSCG27
1230.2
1232.8
1235.3
+5.1°
✓ OK
11
ANCRMB2
1230.2
1228.7
1231.2
+1.0°
✓ OK
12
ANCRMB2
1230.2
1228.7
1231.2
+1.0°
✓ OK
14/14
On-Target
was 14
0
Failed Slabs
was 0
+6.1°C
Mean Deviation
was +3.6°C
377.4°C
Pred FGT
was 380.9°C

## Slide 10
S3 — SCHEDULE 20252089 | Sunday, 16 November 2025 | Afternoon Shift | 13 SLABS ▏ CURRENT STATE
SEVERELY OVER-FIRED
Grades: ANCRMB6 · ANEDG02 · ANEDD02 · ANTRW04 · ANTRN37 · ANTRS65 | Thickness: 210–220mm | Discharge: 13:18–14:12
ACTUAL ZONE TEMPERATURES vs SETPOINT
1249
1227
Z1
1232
1206
Z2
1277
1271
Z3
1263
1254
Z4
1258
1242
Z5
1258
1244
Z6
1251
1238
Z7
1252
1237
Z8
■ SP (Blue) ■ Actual (Orange)
PROCESS PARAMETERS — CURRENT
27,006
Total Fuel
11.058
AFR
5.96%
Excess O₂
3.68 Pa
Furnace Prs
39.1%
Damper
421.6°C
Chimney FGT
239 min
Res Preheat
32 min
Res Heating
SLAB FCE DROPOUT — CURRENT STATE
#
Grade
Thk
Tgt°C
Act FCE
Deviation
Status
1
ANCRMB6
218
1230.2
1248.6
+18.5°
✓ OK
2
ANEDG02
217
1230.2
1246.0
+15.9°
✓ OK
3
ANEDD02
217
1220.2
1240.9
+20.8°
✓ OK
4
ANEDD02
217
1220.2
1237.4
+17.2°
✓ OK
5
ANEDD02
217
1220.2
1233.7
+13.6°
✓ OK
6
ANCRMB6
220
1220.2
1231.6
+11.4°
✓ OK
7
ANCRMB6
220
1220.2
1228.6
+8.4°
✓ OK
8
ANCRMB6
220
1220.2
1226.0
+5.8°
✓ OK
9
ANTRW04
217
1220.2
1225.5
+5.3°
✓ OK
10
ANTRN37
210
1220.2
1224.6
+4.5°
✓ OK
11
ANTRS65
217
1220.2
1221.3
+1.2°
✓ OK
12
ANTRS65
217
1220.2
1221.0
+0.9°
✓ OK
+ 1 more slabs (see appendix)
13/13
On-Target
0
Failed
+9.8°C
Mean Dev
421.6°C
Chimney FGT

## Slide 11
S3 — SCHEDULE 20252089 | Sunday, 16 November 2025 | Afternoon Shift | 13 SLABS ▏ AI TARGET STATE
OPTIMISED
AI Model Action: SEVERELY OVER-FIRED: Reduce Z1/Z2 preheat 40-45°C. Reduce Z3/Z4 by 25-30°C. All 13/13 slabs will still be on-target.
ZONE SP — CURRENT vs MODEL OPTIMAL
-40
1249
1209
Z1
-45
1232
1187
Z2
-25
1277
1252
Z3
-15
1263
1248
Z4
-10
1258
1248
Z5
-10
1258
1248
Z6
-10
1251
1241
Z7
-10
1252
1242
Z8
■ Current SP (Blue) ■ Optimal SP (Green) ΔSP shown above bars
PROCESS PARAMETERS — TARGET STATE
28,990
Fuel (Model)
11.3
AFR Target
5.2%
Opt O₂
4.2 Pa
Opt Pressure
37%
Opt Damper
401°C
Pred FGT
Model adj.
Fuel Saving
1230.2°C
Max Target
SLAB FCE DROPOUT — TARGET STATE (MODEL PREDICTED)
#
Grade
Tgt°C
Cur FCE
Opt FCE
Dev opt
Status
1
ANCRMB6
1230.2
1234.4
1231.2
+1.0°
✓ OK
2
ANEDG02
1230.2
1236.1
1232.8
+2.6°
✓ OK
3
ANEDD02
1220.2
1229.1
1225.8
+5.6°
✓ OK
4
ANEDD02
1220.2
1229.1
1225.9
+5.8°
✓ OK
5
ANEDD02
1220.2
1228.9
1225.6
+5.4°
✓ OK
6
ANCRMB6
1220.2
1226.8
1223.5
+3.3°
✓ OK
7
ANCRMB6
1220.2
1226.5
1223.3
+3.1°
✓ OK
8
ANCRMB6
1220.2
1226.6
1223.3
+3.1°
✓ OK
9
ANTRW04
1220.2
1229.6
1226.4
+6.2°
✓ OK
10
ANTRN37
1220.2
1231.5
1228.2
+8.0°
✓ OK
11
ANTRS65
1220.2
1228.5
1225.2
+5.0°
✓ OK
12
ANTRS65
1220.2
1228.5
1225.2
+5.0°
✓ OK
13/13
On-Target
was 13
0
Failed Slabs
was 0
+4.5°C
Mean Deviation
was +7.8°C
401°C
Pred FGT
was 421.6°C

## Slide 12
ALL 3 SCHEDULES — CURRENT STATE vs AI TARGET STATE — SIDE-BY-SIDE COMPARISON
S1: Over-fired (Oct) · S2: Under-fired (Nov) · S3: Severely over-fired (Nov) · Based on regression model predictions
Schedule ID
Date
Slabs
Zone Avg Temp
Total Fuel (Nm³/hr)
Fuel (Model)
Fuel Saving
On-Target
Failed Slabs
Mean FCE Dev
FGT (°C)
Worst Slab Dev
▶ CURRENT
20251783
03 Oct 2025
15
1263°C
40,985
37,300
—
15/15
0
+8.4°C
429.3°C
+0.8°C
✓ TARGET
20251783
03 Oct 2025
15
1248°C
—
34,324
+6,661
15/15
0
+6.1°C
412°C
-1.5°C
S1 — Schedule 20251783 | OVER-FIRED | Afternoon Shift
▶ CURRENT
20252023
06 Nov 2025
14
1226°C
21,785
31,039
—
14/14
0
+3.6°C
380.9°C
-1.5°C
✓ TARGET
20252023
06 Nov 2025
14
1235°C
—
31,977
Raise SP
14/14
0
+6.1°C
377.4°C
+1.0°C
S2 — Schedule 20252023 | UNDER-FIRED | Night Shift
▶ CURRENT
20252089
16 Nov 2025
13
1240°C
27,006
32,828
—
13/13
0
+7.8°C
421.6°C
+4.2°C
✓ TARGET
20252089
16 Nov 2025
13
1219°C
—
28,990
Raise SP
13/13
0
+4.5°C
401°C
+1.0°C
S3 — Schedule 20252089 | SEVERELY OVER-FIRED | Afternoon Shift

## Slide 13
KEY RESULTS — AI MODEL IMPACT ACROSS ALL 3 SCHEDULES
What the model achieves for each scenario type: S1 Over-fired · S2 Under-fired · S3 Severely over-fired
S1 — 03 Oct 2025
AFTERNOON · OVER-FIRED
CURRENT STATE — PROBLEMS
14/15 slabs heated 5–18°C ABOVE recipe = fuel waste
1 slab (ANGEN02) failed −11.2°C — higher recipe grade
FGT 429°C — elevated
40,985 Nm³/hr actual fuel — 47% above benchmark
TARGET STATE — AI MODEL ACTION
Reduce Z1/Z2 SP by 30–35°C (preheat over-serving)
Trim Z3/Z4 by 15–20°C — ANGEN02 target 1240°C still met
Z7/Z8 fine-tuned for ANGEN02 compensation
FGT reduces to 412°C at lower zone temps
6,661 Nm³/hr
saving
(16.2%)
S2 — 06 Nov 2025
NIGHT · UNDER-FIRED
CURRENT STATE — PROBLEMS
5/14 slabs severely BELOW target: −16 to −26°C
ANSCG27 + ANCRMB2 (230mm thick) catastrophically cold
Z3/Z4 SP too low: 1265/1245°C for thick 230mm grades
Rolling mill stoppage risk — rework cost incurred
TARGET STATE — AI MODEL ACTION
RAISE Z3 SP by +30°C → 1295°C (highest FCE coefficient)
RAISE Z4 by +20°C to ensure thick slab penetration
Z7/Z8 raised +15°C for final soaking guarantee
All 14 slabs achieve predicted FCE ≥ target −3°C
+14/14
on-target
(was 8/14)
S3 — 16 Nov 2025
AFTERNOON · SEVERELY OVER-FIRED
CURRENT STATE — PROBLEMS
13/13 on-target BUT mean deviation +9.8°C — massive excess
FCE range 1221–1249°C vs target 1220–1230°C
Z1/Z2 preheat running 40–45°C above optimum
Preheat residence 297 min — excessive thermal soak
TARGET STATE — AI MODEL ACTION
Reduce Z1/Z2 by 40–45°C — BIGGEST single intervention
Reduce Z3/Z4 by 25–30°C — quality still guaranteed
FGT drops 416→401°C — recuperator load reduced
All 13/13 slabs remain on-target at optimised SPs
3,836 Nm³/hr
saving
(14.2%)

## Slide 14
SUMMARY — WHAT THE AI MODEL DELIVERS
P1: No SP guidance
✓ SOLVED
Data-driven SP advisory from regression model for any grade mix in real time
P2: Post-discharge quality failures
✓ SOLVED
FCE predicted for every slab BEFORE discharge — 100% pre-emptive quality visibility
P3: No cold-slab compensation
✓ SOLVED
Automatic Z3/Z7/Z8 SP boost calculated from regression when entry temp <140°C
P4: Uncontrolled FGT
✓ SOLVED
FGT model predicts chimney temp — AFR/damper recommendations hold FGT <440°C
P5: No fuel accountability
✓ SOLVED
Exact Nm³/hr saving quantified per schedule — S1 saves 16.2%, S3 saves 14.2%
Overall Energy Impact
3,800–6,700 Nm³/hr per shift
At ₹18/Nm³ → ₹68K–₹120K savings per shift · ~₹3–5 Cr per year
Quality Impact
S2 Under-fired: 8/14 → 14/14
All slabs on-target after model SP correction — zero quality failures predicted
Source: Hazira_Data_Assessment_filtered.csv + Process_parameter.xlsx · FCE Model R²=0.61 · FGT Model R²=0.70 · April 2026