## Slide 1
REHEATING FURNACE — ZONE SETPOINT OPTIMIZATION
Energy Gap: Current Actual vs Max Setpoint vs Weighted Average
Hazira Plant · RHF#1 · Nov 2025–Jan 2026 · 6 Production Schedules · 601 Slabs Analysed
CURRENT ACTUAL
What the furnace IS doing today. FCE dropout temperatures, gas consumed, overheating events.
M1 — MAX SETPOINT
Zone set to highest recipe temp in furnace. Safe but over-heats all lower-T grades systematically.
M2 — WEIGHTED AVG
Zone set to mass-weighted recipe avg + 5°C buffer. Energy optimised while maintaining quality.
10.8°C
Avg FCE Excess
over M2 target
70%
Slabs Overheated
>10°C above recipe
~507
NM3/HR Saving
per schedule (avg)
4.7%
Fuel Reduction
M2 vs current
607
Slabs Analysed
across 6 schedules
CONSULTANT'S THESIS: Current furnace operation consumes 1.1–7.2% MORE fuel than necessary in 5 of 6 schedules, due to operating at Max Setpoint irrespective of actual grade mix. Weighted Average model delivers the same product quality at lower energy cost.
Prepared: Independent Technical Consultant · Steel Process Optimisation
CONFIDENTIAL — FOR MANAGEMENT REVIEW

## Slide 2
SCHEDULE COMPARISON — Current · M1 Max · M2 Weighted Average
6 Schedules · 601 Slabs
Chart: FCE/Setpoint Temperature (°C) — All Models
| S19 | S21 | S17 | S18 | S14 | S16
Current FCE Actual | 1243.2 | 1244 | 1246.8 | 1250 | 1231.8 | 1237.6
M1 Max Setpoint | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1230.2
M2 Wtd Avg +5°C | 1233.3 | 1231.3 | 1233.8 | 1236.6 | 1232.1 | 1233.5
Schedule Metrics
Sched | FCE Actual | M1 Max | M2 WtAvg | Excess (°C) | Saving (%)
S19 | 1243.2 | 1240.2 | 1233.3 | +12.0 | 5.2%
S21 | 1244.0 | 1240.2 | 1231.3 | +14.8 | 6.1%
S17 | 1246.8 | 1240.2 | 1233.8 | +15.0 | 7.2%
S18 | 1250.0 | 1240.2 | 1236.6 | +15.4 | 6.4%
S14 | 1231.8 | 1240.2 | 1232.1 | +1.7 | 1.1%
S16 | 1237.6 | 1230.2 | 1233.5 | +6.1 | 2.4%
5 of 6 schedules: FCE is 6–15°C ABOVE the weighted-average recipe target → systematic over-firing
M2 model reduces setpoint by avg 6°C → saves 1–7% fuel with maintained quality via 5°C buffer
Schedule 20260016: only case where M1 < M2 — weighted avg pulled higher. M1 preferred here

## Slide 3
ENERGY GAP ANALYSIS — Current State to Target (M2)
Consultant Quantification
Chart: Gas Saving (NM3/HR): Current → M2 Weighted Average
| S19 | S21 | S17 | S18 | S14 | S16
Gas Saving vs Current (NM3/HR) | 640 | 681 | 695 | 713 | 93 | 222
Chart: Overheated & Under-heated Slabs (%)
| S19 | S21 | S17 | S18 | S14 | S16
Overheated Slabs (%) | 70.6 | 84.5 | 82.4 | 91.1 | 39.6 | 52.1
Under-heated (%) | 13.8 | 3.9 | 9.8 | 0 | 20.8 | 9.4
DETAILED ENERGY SAVINGS — Per Schedule
Schedule | Slabs | Current FCE (°C) | M2 Target FCE (°C) | Excess (°C) | Current Gas (NM3/HR) | Saving (NM3/HR) | Saving (%) | Cost Saving (₹ Lakh) | Overheated Slabs
S19 | 109 | 1243.2 | 1231.3 | +12.0°C | 12,392 | 640 | 5.2% | ₹0.87 | 70.6%
S21 | 103 | 1244.0 | 1229.3 | +14.8°C | 15,717 | 681 | 6.1% | ₹0.88 | 84.5%
S17 | 102 | 1246.8 | 1231.8 | +15.0°C | 11,406 | 695 | 7.2% | ₹0.89 | 82.4%
S18 | 101 | 1250.0 | 1234.6 | +15.4°C | 12,970 | 713 | 6.4% | ₹0.9 | 91.1%
S14 | 96 | 1231.8 | 1230.1 | +1.7°C | 8,328 | 93 | 1.1% | ₹0.11 | 39.6%
S16 | 96 | 1237.6 | 1231.5 | +6.1°C | 13,976 | 222 | 2.4% | ₹0.27 | 52.1%

## Slide 4
ZONE TEMPERATURE PROFILE — All Models Compared
Schedule 20260018 example
Chart: Zone Setpoint (°C) by Zone — Schedule 20260018
| Z1 | Z2 | Z3 | Z4 | Z5 | Z6 | Z7 | Z8
Actual Zone Temp | 1248 | 1262 | 1312 | 1310 | 1280 | 1266 | 1282 | 1265
M1 Max Setpt Zones | 1246.1 | 1243.2 | 1317.6 | 1311.1 | 1257.8 | 1254.3 | 1256.9 | 1247.8
M2 WtAvg Zones | 1242.5 | 1239.6 | 1314 | 1307.5 | 1254.2 | 1250.7 | 1253.3 | 1244.2
Current FCE Dropout | 1250 | 1250 | 1250 | 1250 | 1250 | 1250 | 1250 | 1250
Max Recipe Target | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1240.2 | 1240.2
Zone Setpoints (°C)
Zone | Actual (°C) | M1 (°C) | M2 (°C) | Saving (A→M2)
Z1 | 1248 | 1246 | 1243 | +6°C
Z2 | 1262 | 1243 | 1240 | +22°C
Z3 | 1312 | 1318 | 1314 | -2°C
Z4 | 1310 | 1311 | 1308 | +3°C
Z5 | 1280 | 1258 | 1254 | +26°C
Z6 | 1266 | 1254 | 1251 | +15°C
Z7 | 1282 | 1257 | 1253 | +29°C
Z8 | 1265 | 1248 | 1244 | +21°C
FCE | 1250.0 | 1240.2 | 1234.6 | +15.4°C
ℹ Z8 (Equalising) appears ≤ FCE dropout — CORRECT physics. Slab retains heat from Z3/Z4 soaking zones (+77/+71°C). Z8 homogenises top-bottom temp before discharge. FCE = slab surface temp at exit, driven by stored soaking heat — not Z8 atmosphere.
CONSULTANT NOTE: The 'Actual Zone Temp' shows current furnace is running hotter than even M1 suggests in most zones. This confirms the furnace setpoints are NOT being managed to recipe — a direct control gap that the M2 model addresses.

## Slide 5
MODEL LOGIC — How Each Model Computes Zone Setpoints
CURRENT ACTUAL
Formula:
Setpoint ≈ FCE Dropout Temperature observed
HOW IT WORKS:
Furnace runs at historic/manual setpoints
Zone temperatures reflect operator judgement, not recipe logic
FCE averages 6–15°C above weighted avg recipe target
No systematic adjustment for grade mix changes
Result: 39–91% of slabs are overheated across schedules
VERDICT
❌ Not optimised — over-fires all grades for majority of schedule duration
M1 — MAX SETPOINT
Formula:
SP = max(Recipe₁, Recipe₂, ... , Recipeₙ)
HOW IT WORKS:
Identify highest recipe temp among ALL slabs in furnace
Set all 8 zone targets to: SP + zone-specific offset
Offsets: Z3 +77°C, Z4 +71°C, Z5–Z7 +15–18°C, Z1/Z8 +6–8°C
Every slab guaranteed to reach its recipe temperature
All lower-recipe grades heated to max — not their own recipe
VERDICT
✓ Quality safe but systematically overheats lower-T grades by full spread (up to 20°C)
M2 — WEIGHTED AVERAGE
Formula:
SP = Σ(Massᵢ × Recipeᵢ) / ΣMassᵢ + 5°C safety buffer
HOW IT WORKS:
Compute mass-weighted average of all recipe temps in furnace
Add 5°C safety buffer above raw weighted average
Zone setpoints = SP + same zone-specific offsets as M1
Lower setpoint reduces gas to Z1 & Z2 (66% of total energy)
Override: if any grade recipe > wtavg+10°C, zone boost applied
VERDICT
✓ Energy optimised · 1–7% fuel saving · Quality maintained via buffer

## Slide 6
CONSULTANT RECOMMENDATIONS & IMPLEMENTATION PATH
Based on 6 production schedules, 601 slabs, Nov 2025–Jan 2026
R1
IMMEDIATE ACTION
Adopt M2 (Weighted Average) as Default Setpoint Model
For all schedules with recipe spread <20°C and no new grades under trial, compute mass-weighted average recipe and add 5°C buffer. This single change eliminates 70–91% over-firing in affected schedules. Expected saving: 1–7% fuel per schedule.
R2
CONTROL IMPROVEMENT
Implement Real-time Grade Mix Tracking
Connect L2 schedule system to furnace setpoint controller. At each slab charge event, recompute weighted average of all slabs currently in furnace. Update zone setpoints automatically. Current gap: operators set zones manually to max recipe without grade-mix visibility.
R3
QUALITY SAFEGUARD
Retain M1 Override for Specific Scenarios
Keep M1 (Max Setpoint) active when: (a) recipe spread exceeds 20°C, (b) under-heating events >10% of slabs in prior schedule, (c) new grade introduction, (d) after maintenance downtime. Auto-switching logic between M1 and M2 based on these criteria.
R4
MONITORING
Track P5/P25/P75/P95 of FCE vs Recipe Gap Monthly
Replace single-point FCE target with a distribution-based KPI. Target: P5–P95 FCE band ≤20°C (current: 51°C). Track % slabs overheated by >10°C and % below recipe. Monthly management report comparing M1, M2 and actual performance.